## Slide 1: The Difference Electron Density Map as a Crystal Structure Validation Tool
Ton Spek
Utrecht University
The Netherlands
Vienna-2019-GIG-21-8-2019

## Slide 2: Structure Determination Today
Structure determination programs such as SHELXT, OLEX2 etc. have made structure determination and refinement trivial in many cases.
Problems with a structure may turn up only at the validation stage as IUCr checkCIF ALERTS
Some ALERT messages will need detailed inspection of the difference density map rather than inspection of the residual density peak list.

## Slide 3: Difference Density Map (Fo-Fc)
A good structure model should show no significant residual density excursions > 0.5 eÅ-3
In a good structure model, the value of |ρmin| should be about that of ρmax
Examples follow:

## Slide 4: (Fo-Fc)map for a Healthy Structure
Density on Bonds for a Quality Structure
Reported as a G-ALERT (Info)

## Slide 5: Special Cases
Absence of nice residual density blobs on bonds may indicate:
1 – Poor data associated with high R-value
2 – The use of non-spherical scattering factors E.g. with IDEAL type refinement packages to handle bonding effects
3 – Fraud with calculated ‘ observed’ data. Several cases have now been identified.

## Slide 6
(Fo-Fc) map of an Unhealthy / Wrong Structure
Red: To much density in model; Green: To little density in model
Wrongly Assigned Atom types ?

## Slide 7
False Co-Complex === Zn-Complex
Contours at 0.1 e/Å3
Fraud or Mis-Interpretation

## Slide 8: Wrong Hydrogen Atom Positions
Red:
Too much
density
In model
Green:
Too little
density
In model
Could be caused by wrong AFIX constraint type

## Slide 9: Residual Density Peaks may also point to
Unaccounted for disorder in the molecule(s)
Unaccounted for Twinning (ghost structure peaks)
Absorption artefacts (insufficient correction)
Difficult to model disordered solvents.
Sites occupied by a mixture of solvents

## Slide 10: Warning
Some software will not list residual density peaks on atom sites
Peak search algorithms assume 3D Gaussian type density maxima. Ridges of density might be missed
It is good to inspect the density in solvent accessible voids in a structure.

## Slide 11
Uninterpretable Solvent Channel

## Slide 12
Radius ~ 2

## Slide 13: Heavy Atoms
A peak list often includes density peaks near heavy atoms
Their reason should be investigated
They are often falsely designated as diffraction ripple effects

## Slide 14: Absorption Artefacts (μ=6.45mm-1)
file:///.file/id=6571367.25963400
Typical Difference map without
Absorption correction
Max density 1.40 eA-3
Slight improvement after multiscan
Absorption correction
Max density 0.80 eA-3

## Slide 15: F(obs) and F(obs)-F(calc) Maps Large peaks in a difference map are not due to truncation ripples
Br
Br
Note the truncation ripples in the F(obs) map and absence in the F(obs)-F(calc) map
Fobs Map
Fobs – Fcalc Map

## Slide 16: Example: Validation of a Crystalline Sponge Method based Structure
Fujita et al. (2013) introduced a potentially interesting new approach to obtain structural information for difficult to crystallize compounds
A MOF with suitable channels is used to soak in a molecule of interest for structure determination
Chem. Asian J. (2017), 12, 208-211 provides a good example of a suitable MOF, [CuBr(benzene-1,3,5-triyl-triisonicotinate)]n, soaked with 1-acetonaphthone as guest.

## Slide 17: Replace CS2 with Guest
CS2



Two independent infinite channels A & B (~700 Å3 each)
40%
Solvent
Channel

## Slide 18: Host + Guests in MOF Framework
P21/c
R1 = 0.05
wR2 = 0.18
S = 1.066
Ρmin = -1.26e/Å3
Ρmax = 1.74e/Å3
93K
Guests are:
1-acetonaphthone
CS2

## Slide 19: Refinement
A model with guest molecules and residual CS2 solvent molecules was refined.
Restraints were needed on the geometry
A difference map reveals the reason for the need of those restraints

## Slide 20
A
B
0.1 Å-3
50%Prob.
0.793(4)
0.769(5)
93K
Constraints & Restraints
needed to keep the geometry healthy

## Slide 21: Thanks !